# Tutorials: Dyeing with Food Waste

Overdyeing is the process of dyeing a fabric a darker color to hide stains or discoloration. Many common foods are a great source of natural dyes! This method of overdyeing is a great way to use food waste and reduce textile waste to save stained or faded clothes from the landfill.

Materials needed:

- Garment made of natural fibers, such as 100% cotton or linen (white or light pastel colors will work best)

- Nonreactive (stainless steel) stock pot and lid

- Tongs

- Spoon

- Rubber gloves

- Alum and cream of tartar for mordanting

  - Alternatively, you may use 1/2 cup (150 g) of canning salt for every 8 cups (1.9 L) of water.

- Dye solution made from food scraps (in this example we are using beets, which will be boiled in water to produce a magenta dye and can be eaten afterwards!)

  - How much plant material you need to create your dye depends on how large the item is you are dyeing, and different dye plants will require different amounts to achieve good results.

  - Weigh the item you are dyeing, then collect as much as 50-100% in weight of the stuff you are using to dye with

## Prep Step 1: Scouring (~8hrs)

Scouring cleans the fibers and prepares them to receive the dye.

- Place the fabric in boiling water, adding washing soap (2– 3 tablespoons of washing soda or other gentle soap such as Castille or Olive Oil soap - not detergent or stain blockers).

- Boil for an hour in the solution, and then leave to soak in the solution overnight.

- Rinse well.

## Prep Step 2: Mordanting using alum (24hrs)

Mordanting improves light and color fastness, as well as assists in brighter, clearer colors.

- Add 1 cup of alum and, if available, 2 level tablespoons of cream of tartar to 5 litres (~5 quarts) of water.

- Dissolve the chemicals in warm water and leave fabric to soak for 24 hours.

- Rinse well.

## Step 3: Make the dye solution (~1hr)

Can be done ahead of time while fabric is scouring or mordanting!

- Chop beets into small pieces and place in a pot. You can use a mesh bag or cheesecloth to contain the pieces as desired

- Double the amount of water to plant material (2:1 ratio)

- Bring to a boil then simmer for about an hour or more.

- If making ahead of time, strain & store in a sealed jar out of sunlight until ready to use, otherwise, proceed directly to step 4!

## Step 4: Dyeing (1 - 2 hrs)

- Bring the dye solution to just under boiling temperature and let the mixture simmer, but not actually boil.

- Now add the fabric to the hot dye bath. Stir frequently, Keep the material moving gently to ensure that the dyeing will be even.

- Keep the material in the dye for at least 1hr hour – depending on how strong you want the colour to be. You can leave it for 12-24 hours in the dye bath for best results.

- Remove and let cool.

- Rinse the material several times until the water becomes clear.

- Give a final wash with pH Neutral soap such as Synthropol. Then rinse and dry.

- Let dye set for 1-2 weeks before further washing

Additional Resources:

- Wild Color, Revised and Updated Edition: The Complete Guide to Making and Using Natural Dyes, Jenny Dean

- The Modern Natural Dyer: A Comprehensive Guide to Dyeing Silk, Wool, Linen and Cotton at Home, Kristine Vejar

- Journeys in Natural Dyeing: Techniques for Creating Color at Home, Kristine Vejar

- Harvesting Color: How to Find Plants and Make Natural Dyes, Rebecca Burgess

- Shibori: The Inventive Art of Japanese Shaped Resist Dyeing -  Yoshiko Iwamoto Wada